TWO-PART EPOXY ADHESIVE SYSTEM

MS-907

For bonding metals, glass, ceramics, plastics, wood, rubber, fabrics and concrete.  Miller-Stephenson’s Epoxy 907 Adhesive System is a two-part, equal volume, room temperature curing system particularly useful for general purpose bonding.  Fast set-up time.  Perfect for in-plant and field use.  Develops bond strength to 3,000 psi.

| BONDING STRENGTH | To 3,000 PSI |
| --- | --- |
| FORM | A two-part paste adhesive packaged in equal volume tubes. |
| COLOR | Part A is blue. Part B is beige. When thoroughly mixed, the result is light blue. |
| VISCOSITY | Approximately 120,000 cP, thixotropic. |
| MIX RATIO | Equal parts by volume. |
| POT LIFE | 20 minutes at 77˚F, 200 grams |
| CURE TIME | 24 hours at 77˚F, or 2 hours at 140˚F, or 1 hour at 180˚F. Do not attempt to cure below 60˚F. |
| SERVICE TEMPERATURE | -50˚ to 180˚F |
| SHELF LIFE | More than 1 year at 75˚F. |
| SPECIAL PROPERTIES | Good adhesion to wide variety of surfaces. Color-coded for proper mixing. |

TYPICAL CURED PROPERTIES @ 77˚F(25˚C)

| Tensile Strength, psi (ASTM D 638)…………………………... | 3100 |
| --- | --- |
| Modulus, psi (ASTM D 638)…………………………………… | 245,000 |
| Elongation at Break, % (ASTM D 638)…….…………………… | 2.4 |
| Coefficient of Linear Thermal Expansion, in/in/˚C(ASTM D 696) | 45 x 10-6 |
| Thermal Conductivity Cal Cm/(CM2)(Sec)(˚C) x 10-4…………… | 6.8 |
| % Water Absorption |  |
| 24 Hours……………………………………………………… | 0.66 |
| 7 Days………………………………………………………... | 2.28 |
| Linear Shrinkage, in/in…………………………………………… | 0.00025 |
| Hardness, Shore D……………………………………………….. | 79 |

###### TYPICAL ELECTRICAL PROPERTIES

| Volume Resistivity, Ohm-cm @ 100 volts, 77˚F (25˚C)…………. | 3.16 x 1014 |
| --- | --- |
| Dielectric Constant, MIL 1-16923. K 1kHz……………………... | 4.58 |
| Dissipation Factor, ASTM D 150 1kHz……………………….. | 0.076 |

###### TYPICAL TENSILE BOND STRENGTH

Typical tensile shear strengths for bonds to etched aluminum (ASTM D 1002), cured 24 hours at 77˚F are:

| Test Temperature, ˚F | Tensile Shear Strength, PSI |
| --- | --- |
| -67 | 2300 |
| 77 | 3000 |
| 180 | 1000 |
| 250 | 400 |

Typical tensile bond strength obtained at room temperature with various MEK wiped substrates are as follows:

| Substrate PSI @ 75˚F | Substrate PSI @ 75˚F |
| --- | --- |
| Galvanized steel 1800 | Epoxy laminate 400 |
| Bonderized steel 1900 | Plate glass 1100 |
| Black iron 2200 | Penton 600 |
| Tin plate 1300 | Polyethylene 500 |
| Terne plate 1200 | Polypropylene 400 |
| Brass 500 | Plexiglas® 200 |
| Copper 1000 | Hi-impact polystyrene 0 |
| Alclad 3000 | CaCO3 filled buna rubber 300 |
| Polyester laminate 800 | Neoprene 500 |

Plexiglas ® is a registered trademark of Atoglas Co.

###### DIRECTIONS

- CLEAN SURFACES Surfaces to be bonded must be clean, dry and free of oil,

grease or wax.  Roughen nonporous surfaces with sandpaper or emery paper for hard materials.

- MIX EQUAL PARTS Squeeze a length from tube A on a clean, dry, flat

disposable surface.  Use uniform pressure for even bead.  Parallel to tube A, run an equal length bead from tube B.

- MIX THOROUGHLY Important!  Mix the two beads together for 3 minutes or

longer.  When properly mixed, the adhesive is light blue.

- APPLY TO BOTH SURFACES Cover entire area evenly.

5.	JOIN PARTS TOGETHER FIRMLY Squeeze out excess adhesive to form a

thin glue line.  A larger area will require more pressure.  Hold parts together with

clamps, weights or tape.

- REMOVE EXCESS ADHESIVE PROMPTLY Before adhesive hardens,

scrape with putty knife.  Clean with lacquer thinner, acetone or turpentine.  Once cured, adhesive may be removed by sanding.

1483-4C